CODING

SETS

j       raw materials           / Limestone, Clay, Sand, Fe_Source                   /

k       fossil fuels            / Coal, Pet_Coke                                     /

l       non fossil fuels        / RDF, Sewage_Sludge, TDF, MBM                       /

o       oxides                  / SiO2, Al2O3, Fe2O3, CaO, MgO                       /

a       alkalis                 / K2O, Na2O                                          /

s       sulfurs                 / SO3                                                /

g       flue gases              / CO2, N2, O2, H2O                                   /

h       heavy metals            / NiO, V2O5, ZnO, Cd, Pb, Tl, As, Hg                 /

p       clinker phases          / C3S, C2S, C3A, C4AF                                /

c       ccs                     / Post_Comb, Pre_Comb                                /

r       kiln                    / Refractories, Control, Stages                      /

*         r       kiln                    / Refractories, Control, Combustion, Stages          /

;

PARAMETER

*++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++

****RAW MATERIALS**RAW MATERIALS**RAW MATERIALS**RAW MATERIALS**RAW MATERIALS****

*++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++

*Clinker phases formed by oxides for raw materials j

*wt/wt%

MgO_j(j)           mass ratio of MgO in raw materials j

/       Limestone       0.005

Clay            0.123

Sand            0.020

Fe_Source       0.010   /

*wt/wt%

SiO2_j(j)          mass ratio of SiO2 in raw materials j

/       Limestone       0.1000

Clay            0.4956

Sand            0.8000

Fe_Source       0.0100  /

*wt/wt%

Fe2O3_j(j)         mass ratio of Fe2O3 in from raw materials j

/       Limestone       0.0100

Clay            0.1073

Sand            0.0250

Fe_Source       0.9500  /

*wt/wt%

Al2O3_j(j)         mass ratio of Al2O3 in raw materials j

/       Limestone       0.0100

Clay            0.1041

Sand            0.0500

Fe_Source       0.0050  /

*wt/wt%

CaO_j(j)           mass ratio of CaO in raw materials j

/       Limestone       0.5000

Clay            0.0400

Sand            0.0382

Fe_Source       0.0200  /

*wt/wt%

K2O_j(j)            mass ratio of K2O in raw materials j

/       Limestone       0.0030

Clay            0.0022

Sand            0.0150

Fe_Source       0.0010  /

*wt/wt%

Na2O_j(j)            mass ratio of K2O in raw materials j

/       Limestone       0.0010

Clay            0.0139

Sand            0.0050

Fe_Source       0.0010  /

*wt/wt%

SO3_j(j)            mass ratio of SO3 in raw materials j

/       Limestone       0.0001

Clay            0.0010

Sand            0.0005

Fe_Source       0.0030  /

*++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++

**FOSSIL FUELS*FOSSIL FUELS*FOSSIL FUELS*FOSSIL FUELS*FOSSIL FUELS*FOSSIL FUELS**

*++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++

*Clinker phases formed by oxides for fossil fuels k

*wt/wt%

SiO2_k(k)          mass ratio of SiO2 in ash of fossil fuels k

/       Coal            0.5250

Pet_Coke        0.4000  /

*wt/wt%

Fe2O3_k(k)         mass ratio of Fe2O3 in ash of fossil fuels k

/       Coal            0.1000

Pet_Coke        0.0700  /

*wt/wt%

Al2O3_k(k)         mass ratio of Al2O3 in ash of fossil fuels k

/       Coal            0.3000

Pet_Coke        0.1000  /

*wt/wt%

CaO_k(k)           mass ratio of CaO in ash of fossil fuels k

/       Coal            0.0300

Pet_Coke        0.0100  /

*wt/wt%

K2O_k(k)           mass ratio of K2O in ash of fossil fuels k

/       Coal            0.0150

Pet_Coke        0.0050  /

*wt/wt%

Na2O_k(k)           mass ratio of Na2O in ash of fossil fuels k

/       Coal            0.0050

Pet_Coke        0.0050  /

*wt/wt%

SO3_k(k)           mass ratio of SO3 in ash of fossil fuels k

/       Coal            0.0150

Pet_Coke        0.0200  /

*wt/wt%

fraction_h_k(k)    mass fraction of hydrogen h from fossil fuels k

/       Coal            0.050

Pet_Coke        0.030   /

*Random coefficients values for fossil fuels k

*wt/wt%

ash_k(k)           mass fraction of ash in fossil fuels k

/       Coal            0.10

Pet_Coke        0.01    /

*kJ/kg fuel

*NCV_k(k)           net calorific value for fossil fuels k

*                 /       Coal            30000

*                         Pet_Coke        33000   /

*GJ/kg fuel

NCV_k(k)           net calorific value for fossil fuels k

/       Coal            0.030

Pet_Coke        0.033   /

CEF_k(k)           carbon emission factor for fossil fuels k

/       Coal            2.75

Pet_Coke        3.3    /

anthro_k(k)        mass fraction of biogenic carbon emission from fossil fuels k

/       Coal            0

Pet_Coke        0       /

*Atomic mass fraction for fossil fuels k

*wt/wt%

atom_C_k(k)          atom C mass fraction of fossil fuels k

/       Coal            0.75

Pet_Coke        0.90    /

*wt/wt%

atom_H_k(k)          atom H mass fraction of fossil fuels k

/       Coal            0.05

Pet_Coke        0.03    /

*wt/wt%

atom_O_k(k)          atom O mass fraction of fossil fuels k

/       Coal            0.08

Pet_Coke        0.01    /

*wt/wt%

atom_S_k(k)          atom S mass fraction of fossil fuels k

/       Coal            0.003

Pet_Coke        0.040   /

St_O2_k(k)           stoichiometric O2 of fossil fuels k

/       Coal            2.325

Pet_Coke        2.690   /

*++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++

***NON FOSSIL FUELS***NON FOSSIL FUELS*****NON FOSSIL FUELS***NON FOSSIL FUELS***

*++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++

*Clinker phases formed by oxides for non fossil fuels l

*wt/wt%

SiO2_l(l)          mass ratio of SiO2 in ash of non fossil fuels l

/       RDF             0.4000

Sewage_Sludge   0.4000

TDF             0.2200

MBM             0.0050  /

*wt/wt%

Fe2O3_l(l)         mass ratio of Fe2O3 in ash of non fossil fuels l

/       RDF             0.0200

Sewage_Sludge   0.0500

TDF             0.0150

MBM             0.0000  /

*wt/wt%

Al2O3_l(l)         mass ratio of Al2O3 in ash of non fossil fuels l

/       RDF             0.2500

Sewage_Sludge   0.1500

TDF             0.1000

MBM             0.0000  /

*wt/wt%

CaO_l(l)           mass ratio of CaO in ash of non fossil fuels l

/       RDF             0.2000

Sewage_Sludge   0.2000

TDF             0.1100

MBM             0.2000  /

*wt/wt%

K2O_l(l)           mass ratio of K2O in ash of non fossil fuels l

/       RDF             0.0100

Sewage_Sludge   0.0100

TDF             0.0100

MBM             0.0050  /

*wt/wt%

Na2O_l(l)           mass ratio of Na2O in ash of non fossil fuels l

/       RDF             0.0100

Sewage_Sludge   0.0100

TDF             0.0100

MBM             0.0000  /

*wt/wt%

SO3_l(l)           mass ratio of SO3 in ash of non fossil fuels l

/       RDF             0.0200

Sewage_Sludge   0.0100

TDF             0.1500

MBM             0.0000  /

*wt/wt%

fraction_h_l(l)    mass fraction of hydrogen h from non fossil fuels l

/       RDF             0.100

Sewage_Sludge   0.090

TDF             0.07

MBM             0.06    /

*Random coefficients values for non fossil fuels l

*wt/wt%

ash_l(l)           mass fraction of ash in non fossil fuels l

/       RDF             0.10

Sewage_Sludge   0.20

TDF             0.10

MBM             0.30    /

*kJ/kg fuel

*NCV_l(l)           net calorific value for non fossil fuels l

*                 /       RDF             26000

*                         Sewage_Sludge   16000

*                         TDF             32000

*                         MBM             17000   /

*GJ/kg fuel

NCV_l(l)           net calorific value for non fossil fuels l

/       RDF             0.026

Sewage_Sludge   0.016

TDF             0.032

MBM             0.017   /

CEF_l(l)           carbon emission factor for non fossil fuels l

/       RDF             2.2

Sewage_Sludge   1.58

TDF             2.56

MBM             1.54    /

anthro_l(l)        mass fraction of biogenic carbon emission from non fossil fuels l

/       RDF             0.5

Sewage_Sludge   0.5

TDF             0

MBM             1       /

*atom mass fraction for non fossil fuels l

*wt/wt%

atom_C_l(l)          atom C mass fraction of non fossil fuels l

/       RDF             0.60

Sewage_Sludge   0.43

TDF             0.70

MBM             0.42    /

*wt/wt%

atom_H_l(l)          atom H mass fraction of non fossil fuels l

/       RDF             0.10

Sewage_Sludge   0.09

TDF             0.07

MBM             0.06    /

*wt/wt%

atom_O_l(l)          atom O mass fraction of non fossil fuels l

/       RDF             0.250

Sewage_Sludge   0.272

TDF             0.100

MBM             0.153   /

*wt/wt%

atom_S_l(l)          atom S mass fraction of non fossil fuels l

/       RDF             0.010

Sewage_Sludge   0.002

TDF             0.015

MBM             0.004    /

St_O2_l(l)           stoichiometric O2 of non fossil fuels l

/       RDF             2.165

Sewage_Sludge   1.598

TDF             2.349

MBM             1.453    /

*++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++

*FLUE GAS**FLUE GAS**FLUE GAS**FLUE GAS***FLUE GAS**FLUE GAS**FLUE GAS**FLUE GAS*

*++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++

molecular_flue(g)        molecular weight for flue gas g

/       CO2             44.01

N2              28.0134

O2              31.9988

H2O             18.0153  /

*++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++

*KILN*KILN*KILN*KILN*KILN*KILN*KILN*KILN*KILN*KILN*KILN*KILN*KILN*KILN*KILN*KILN*

*++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++

*%

*effect_r(r)              reduced thermal energy when mitigation technology r in kiln is installed

*                  /      Refractories    0.193846154

*                         Control         0.061538462

*                         Combustion      0.153846154

*                         Stages          0.030769231  /

*%

*effect_r(r)              reduced thermal energy when mitigation technology r in kiln is installed

*                  /      Refractories    0.194

*                         Control         0.062

*                         Combustion      0.154

*                         Stages          0.031  /

*%

effect_r(r)              reduced thermal energy when mitigation technology r in kiln is installed

/      Refractories    0.193846154

Control         0.061538462

Stages          0.030769231   /

*%

*effect_r(r)              reduced thermal energy when mitigation technology r in kiln is installed

*                  /      Refractories    0.194

*                         Control         0.062

*                         Stages          0.031  /

*++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++

*CCS*CCS*CCS*CCS*CCS*CCS*CCS*CCS*CCS*CCS*CCS*CCS*CCS*CCS*CCS*CCS*CCS*CCS*CCS*CCS*

*++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++

effect_c(c)              CO2 mitigated when carbon capture and storage c is installed

/       Post_Comb       0.98

Pre_Comb        0.61       /

n_oxy(c)                 effect from oxyfuel CCS selection

/       Post_Comb       0

Pre_Comb        1          /

*++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++

****RAW MATERIALS**RAW MATERIALS**RAW MATERIALS**RAW MATERIALS**RAW MATERIALS****

*++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++

*cost for raw materials j

*€/kg

Cost_Raw(j)      cost of raw materials j

/       Limestone       0.01631

Clay            0.03375

Sand            0.00575

Fe_Source       0.01304    /

*++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++

**FOSSIL FUELS*FOSSIL FUELS*FOSSIL FUELS*FOSSIL FUELS*FOSSIL FUELS*FOSSIL FUELS**

*++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++

*cost for fossil fuels k

*€/kg

Cost_Foss(k)     cost of fossil fuels k

/       Coal            0.10

Pet_Coke        0.09       /

*++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++

***NON FOSSIL FUELS***NON FOSSIL FUELS*****NON FOSSIL FUELS***NON FOSSIL FUELS***

*++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++

*cost for non fossil fuels l

*€/kg

Cost_NonFoss(l)  cost of non fossil fuels l

/       RDF             0.05

Sewage_Sludge   0.04

TDF             0.03

MBM             0.02       /

*++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++

*CO-PROCESS**CO-PROCESS**CO-PROCESS**CO-PROCESS**CO-PROCESS*

*++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++

*€/year

Cost_fuel_FCI(l)      capital cost for non fossil fuels l (co-process)

/       RDF             200000

Sewage_Sludge   200000

TDF             300000

MBM             300000        /

*€/kg fuel

Cost_fuel_VC(l)       variable cost for non fossil fuels l (co-process)

/        RDF             0.005

Sewage_Sludge   0.005

TDF             0.010

MBM             0.010      /

*++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++

*KILN*KILN*KILN*KILN*KILN*KILN*KILN*KILN*KILN*KILN*KILN*KILN*KILN*KILN*KILN*KILN*

*++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++

*€/t clinker

*Cost_kiln_FCI(r)         installation cost for mitigation technology r in kiln

*                  /      Refractories    0.23

*                         Control         1.56

*                         Combustion      0.92

*                         Stages          0.81  /

*€/t clinker

Cost_kiln_FCI(r)         installation cost for mitigation technology r in kiln

/      Refractories    0.23

Control         1.56

Stages          0.81  /

*++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++

*CCS*CCS*CCS*CCS*CCS*CCS*CCS*CCS*CCS*CCS*CCS*CCS*CCS*CCS*CCS*CCS*CCS*CCS*CCS*CCS*

*++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++++

*€

Cost_ccs_FCI(c)       capital cost for carbon capture and storage c

/       Post_Comb       190700000

Pre_Comb        46330000        /

*€/y

Cost_ccs_VC(c)        variable cost for carbon capture and storage c

/       Post_Comb       22210000

Pre_Comb        7860000       /

;

*--------------------------------------------------------------------------------

**SCALAR*SCALAR*SCALAR*SCALAR*SCALAR**SCALAR*SCALAR*SCALAR*SCALAR*SCALAR*SCALAR**

*--------------------------------------------------------------------------------

SCALAR   TSR             /   0.30   /

SCALAR   CO2_Target      /   0.04   /

*Case study (Base)

SCALAR   FCI             /264000000/

SCALAR   OC              / 23660000/

SCALAR   AC              / 1000000 /

SCALAR   CCO2            / 880.885 /

SCALAR   Basis           /  1000   /

*SCALAR   TED_Base        / 3500000 /

SCALAR   TED_Base        /   3.5   /

SCALAR   correlate       /   0.95  /

SCALAR   UMC3S           /  0.600  /

SCALAR   UMC2S           /  0.350  /

SCALAR   UMC3A           /  0.150  /

SCALAR   UMC4AF          /  0.150  /

SCALAR   LMC3S           /  0.500  /

SCALAR   LMC2S           /  0.100  /

SCALAR   LMC3A           /  0.010  /

SCALAR   LMC4AF          /  0.010  /

*SCALAR   Amor            / 0.1102  /

SCALAR   Amor            /0.110168072190021/

SCALAR   SO3_flue        / 0.00003 /

;

*--------------------------------------------------------------------------------

**TABLES*TABLES*TABLES*TABLES*TABLES**TABLES*TABLES*TABLES*TABLES*TABLES*TABLES**

*--------------------------------------------------------------------------------

*wt/wt%

TABLE    Raw_Materials_Oxides(o,j)      Mass fraction of oxides o in raw materials j

Limestone       Clay         Sand       Fe_Source

SiO2            0.1000       0.4956       0.8000       0.0100

Al2O3           0.0100       0.1041       0.0500       0.0050

Fe2O3           0.0100       0.1073       0.0250       0.9500

CaO             0.5000       0.0382       0.0300       0.0200

MgO             0.0050       0.1232       0.0200       0.0100

;

*wt/wt%

TABLE    Raw_Materials_Alkalis(a,j)     Mass fraction of alkalis a in raw materials j

Limestone       Clay         Sand       Fe_Source

K2O             0.0030       0.0022       0.0150       0.0010

Na2O            0.0010       0.0139       0.0050       0.0010

;

*wt/wt%

TABLE    Raw_Materials_Sulfurs(s,j)     Mass fraction of sulfurs s in raw materials j

Limestone       Clay         Sand       Fe_Source

SO3             0.0001       0.0010       0.0005       0.0030

;

*wt/wt%

TABLE    Fossil_Fuels_Ash_Oxides(o,k)   Mass fraction of oxides o in ash from fossil fuels k

Coal       Pet_Coke

SiO2            0.5250       0.4000

Al2O3           0.3000       0.1000

Fe2O3           0.1000       0.0700

CaO             0.0300       0.0100

MgO             0.0100       0.0300

;

*wt/wt%

TABLE    Fossil_Fuels_Ash_Alkalis(a,k)   Mass fraction of alkalis a in ash from fossil fuels k

Coal       Pet_Coke

K2O             0.0150       0.0050

Na2O            0.0050       0.0050

;

*wt/wt%

TABLE    Fossil_Fuels_Sulfurs(s,k)   Mass fraction of sulfurs s from fossil fuels k

Coal       Pet_Coke

SO3             0.0030       0.0400

;

*wt/wt%

TABLE    Fossil_Fuels_Ash_Metals(h,k)    Mass fraction of heavy metals h in ash from fossil fuels k

Coal       Pet_Coke

NiO              0.000000     0.150000

V2O5             0.000000     0.200000

ZnO              0.000200     0.000050

Cd               0.000010     0.000001

Pb               0.000200     0.000010

Tl               0.000004     0.000080

As               0.000002     0.000005

Hg               0.000000     0.000000

;

*wt/wt%

TABLE    Non_Fossil_Fuels_Ash_Oxides(o,l)      Mass fraction of oxides o in ash from non fossil fuels l

RDF      Sewage_Sludge     TDF         MBM

SiO2             0.4000       0.4000       0.2200       0.0050

Al2O3            0.2500       0.1500       0.1000       0.0000

Fe2O3            0.0200       0.0500       0.0150       0.0000

CaO              0.2000       0.2000       0.1100       0.2000

MgO              0.0250       0.0250       0.0150       0.0000

;

*wt/wt%

TABLE    Non_Fossil_Fuels_Ash_Alkalis(a,l)     Mass fraction of alkalis a in ash from non fossil fuels l

RDF      Sewage_Sludge     TDF         MBM

K2O              0.0100       0.0100       0.0100       0.0050

Na2O             0.0100       0.0100       0.0100       0.0000

;

*wt/wt%

TABLE    Non_Fossil_Fuels_Sulfurs(s,l)     Mass fraction of sulfurs s in ash from non fossil fuels l

RDF      Sewage_Sludge     TDF         MBM

SO3              0.0100       0.0020       0.0150       0.0040

;

*wt/wt%

TABLE    Non_Fossil_Fuels_Ash_Metals(h,l)    Mass fraction of heavy metals h in ash from non fossil fuels l

RDF      Sewage_Sludge      TDF          MBM

NiO              0.0000000     0.0000000     0.0000000    0.0000000

V2O5             0.0000000     0.0000000     0.0000000    0.0000000

ZnO              0.0000850     0.0007000     0.3500000    0.0000000

Cd               0.0000010     0.0000050     0.0000050    0.0000000

Pb               0.0000500     0.0030000     0.0000500    0.0000000

Tl               0.0000000     0.0000000     0.0000001    0.0000000

As               0.0000050     0.0000200     0.0000001    0.0000000

Hg               0.0000020     0.0000150     0.0000000    0.0000000

;

*wt/wt%

TABLE    Clinker_Phases(p,o)

SiO2         Al2O3        Fe2O3         CaO          MgO

C3S              -7.600       -6.720       -1.430       +4.070       +0.000

C2S              +8.600       +5.070       +1.080       -3.070       +0.000

C3A              +0.000       +2.650       -1.690       +0.000       +0.000

C4AF             +0.000       +0.000       +3.043       +0.000       +0.000

;

*********************************************************************************

*VARIABLES*(III)*VARIABLES*(III)*VARIABLES*(III)*VARIABLES*(III)*VARIABLES*(III)*

*********************************************************************************

VARIABLES

min_cost        minimize cost ;

POSITIVE VARIABLES

m_oxides(o)

m_alkalis(a)

m_sulfurs(s)

m_metals(h)

mass_raw(j)

mass_foss(k)

mass_nonfoss(l)

m_clink

linearize_l(l)

linearize_k(k)

linearize_c(c)

linearize_air(c)

linearize_oxygen(c)

nonbio_CO2

bio_CO2

total_CO2

CO2_released

m_flue_g

m_air

mass_SO3_flue

mass_H2O

mass_O2

mass_N2

m_oxygen

V_flue

mass_clinker_produced

mass_fuels_used

mass_raws_used

produced_CO2

CO2_foss

CO2_nonfoss

CCS

CO2_nonbio_altfuel

CO2_nonbio_fossfuel

oxygen_used

oxygen_feed

CO2_captured

*CCO2

cost_raws

total_raws

cost_fossil

total_fossil

cost_nonfossil

total_nonfossil

total_fuel

nonfossil_overall

cost_coprocess

cost_kiln

cost_ccs

plant_cost

thermal_1

thermal_2

C3S

C2S

C3A

C4AF

annual

capital

;

BINARY VARIABLES

XK(k)

XL(l)

XR(r)

XC(c)

;

*********************************************************************************

**EQUATIONS*(IV)**EQUATIONS*(IV)**EQUATIONS*(IV)**EQUATIONS*(IV)**EQUATIONS*(IV)*

*********************************************************************************

EQUATIONS

obj_fctn

bincons1

bincons2

bincons3

cons1

cons2

cons3

cons4

cons5

cons6

cons7

cons8

cons9

cons10

cons11

cons12

cons13

cons14

cons15

cons16

cons17

cons18

cons19

cons20

cons21

cons22

cons23

cons24

cons25

cons26

cons27

cons28

cons29

cons30

cons31

cons32

cons33

cons34

cons35

cons36

cons37

cons38

cons39

cons40

cons41

cons42

cons43

cons44

cons45

cons46

cons47

cons48

cons49

cons50

cons51

cons52

cons53

cons54

cons55

cons56

cons57

cons58

cons59

cons60

cons61

cons62

cons63

cons64

cons65

cons66

cons67

cons68

cons69

cons70

cons71

cons72

cons73

cons74

cons75

cons76

cons77

;

*------------------------------------------------------------------------------------

* OBJECTIVE FUNCTION * OBJECTIVE FUNCTION * OBJECTIVE FUNCTION * OBJECTIVE FUNCTION *

*------------------------------------------------------------------------------------

*€/t clinker

obj_fctn..       min_cost =e=

*Capital cost

correlate*Amor*FCI/AC + correlate*OC/AC +

*Raw materials j cost

sum (j, Cost_Raw(j)*mass_raw(j)) +

*Fossil fuels k cost

sum (k, Cost_Foss(k)*mass_foss(k)) +

*Non fossil fuels l cost

sum (l, Cost_NonFoss(l)*mass_nonfoss(l)) +

*Retrofitting cost (fuel switching + kiln + CCS retrofitting)

*Kiln

sum (r, (correlate*XR(r)*Cost_kiln_FCI(r))) +

*Fuel switching cost

sum (l, ((correlate*XL(l)*Cost_fuel_FCI(l)/AC) + (Cost_fuel_VC(l)*mass_nonfoss(l)))) +

*CCS installation

sum (c, ((correlate*Amor*Cost_ccs_FCI(c)*XC(c)/AC) + (correlate*Cost_ccs_VC(c)*XC(c)/AC)))

;

*------------------------------------------------------------

* BINARY CONSTRAINT * BINARY CONSTRAINT * BINARY CONSTRAINT *

*------------------------------------------------------------

bincons1..        sum (r, XR(r)) =l= 0

;

*Combination of fuels used must not be more than the maximum amount of fuel that can be fired from multichannel burner

*vintage "3 channel" type burner; 2 fuels and 1 air

bincons2..        sum (k, XK(k)) + sum (l, XL(l)) =l= 2

;

bincons3..        sum (c, XC(c)) =l= 0

;

*----------------------------------------------------------------------------------------------------------------------------------------------------------------------

* EQUALITY CONSTRAINT * EQUALITY CONSTRAINT * EQUALITY CONSTRAINT * EQUALITY CONSTRAINT * EQUALITY CONSTRAINT * EQUALITY CONSTRAINT * EQUALITY CONSTRAINT

*----------------------------------------------------------------------------------------------------------------------------------------------------------------------

*===========================================*

**OVERALL MASS BALANCE FOR CLINKER PRODUCED**

*===========================================*

*kg/t clinker

cons1..          sum (o, m_oxides(o)) + sum (a, m_alkalis(a))

+ sum (s, m_sulfurs(s)) + sum (h, m_metals(h))

=g= Basis

;

*Mass of oxides

*kg/t clinker

cons2(o)..          m_oxides(o) =e=

*Oxides from raw materials j

sum (j, Raw_Materials_Oxides(o,j)*mass_raw(j)) +

*Oxides from ash in fossil fuels k

sum (k, Fossil_Fuels_Ash_Oxides(o,k)*mass_foss(k)*ash_k(k)) +

*Oxides from ash in non fossil fuels l

sum (l, Non_Fossil_Fuels_Ash_Oxides(o,l)*mass_nonfoss(l)*ash_l(l))

;

*Mass of alkalis

*kg/t clinker

cons3(a)..          m_alkalis(a) =e=

*Alkalis from raw materials j

sum (j, Raw_Materials_Alkalis(a,j)*mass_raw(j)) +

*Alkalis from ash in fossil fuels k

sum (k, Fossil_Fuels_Ash_Alkalis(a,k)*mass_foss(k)*ash_k(k)) +

*Alkalis from ash in non fossil fuels l

sum (l, Non_Fossil_Fuels_Ash_Alkalis(a,l)*mass_nonfoss(l)*ash_l(l))

;

*Mass of sulfurs

*kg/t clinker

cons4(s)..          m_sulfurs(s) =e=

*Sulfurs from raw materials j

sum (j, Raw_Materials_Sulfurs(s,j)*mass_raw(j)) +

*Sulfurs from fossil fuels k

sum (k, Fossil_Fuels_Sulfurs(s,k)*mass_foss(k)*(80/32)) + sum (k, SO3_k(k)*ash_k(k)*mass_foss(k)) +

*Sulfurs from non fossil fuels l

sum (l, Non_Fossil_Fuels_Sulfurs(s,l)*mass_nonfoss(l)*(80/32)) + sum (l, SO3_l(l)*ash_l(l)*mass_nonfoss(l))

;

*Mass of heavy metals

*kg/t clinker

cons5(h)..          m_metals(h) =e=

*Metals from ash in fossil fuels k

sum (k, Fossil_Fuels_Ash_Metals(h,k)*mass_foss(k)*ash_k(k)) +

*Metals from ash in non fossil fuels l

sum (l, Non_Fossil_Fuels_Ash_Metals(h,l)*mass_nonfoss(l)*ash_l(l))

;

*kg/t clinker

cons6..            mass_clinker_produced =e=

sum (o, m_oxides(o)) + sum (a, m_alkalis(a)) + sum (s, m_sulfurs(s)) + sum (h, m_metals(h))

;

*=======================================*

**OVERALL MASS BALANCE FOR CO2 PRODUCED**

*=======================================*

*Mass of CO2 emitted can be divided into CO2 emitted by fuels [biogenic fuels (rdf, ss, mbm) and nonbiogenic fuels (coal, pet_coke, tdf)] and emitted by chemicals in kiln

*Non biogenic CO2 emissions

*kg/t clinker

cons7..            nonbio_CO2 =e=

*Mass of CO2 emitted from clinkerization

m_clink +

*Mass of CO2 produced by the burning of fossil fuels k

sum (k, (1 - anthro_k(k))*CEF_k(k)*linearize_k(k)) +

*Mass of CO2 produced by the burning of non fossil fuels l

sum (l, (1 - anthro_l(l))*CEF_l(l)*linearize_l(l))

;

*CO2 emissions from clinkerization

*kg/t clinker

cons8..            m_clink =e=

*Mass of CO2 produced from CaO

((44/56)*sum(j, CaO_j(j)*mass_raw(j))) +

*Mass of CO2 produced from MgO

((44/40)*sum(j, MgO_j(j)*mass_raw(j)))

;

*Biogenic CO2 emissions

*kg/t clinker

cons9..         bio_CO2 =e=

*Mass of CO2 produced by the burning of non fossil fuels l

sum (l, anthro_l(l)*CEF_l(l)*linearize_l(l))

;

*Total CO2

cons10..        produced_CO2 =e=

*non biogenic CO2 emissions

nonbio_CO2 +

*biogenic CO2 emissions

bio_CO2

;

cons11..         CO2_released =e=

*Total CO2

produced_CO2 -

*amount of CO2 reduced by CCS

(sum (c, linearize_c(c)*effect_c(c)))

;

*==============================================*

**OVERALL MASS BALANCE FOR FLUE GASES PRODUCED**

*==============================================*

*Volumetric flowrate of flue gas

*Nm3/t clinker

cons12..         V_flue =e=

22.414*

*Oxygen

((mass_O2/32)+

*Nitrogen

(mass_N2/28)+

*Water vapor

(mass_H2O/18) +

*Carbon dioxide

(produced_CO2/44))

;

*Mass of flue gas

*kg/t clinker

cons13..         m_flue_g =e=

mass_O2 + mass_N2 + mass_H2O + produced_CO2

;

*Mass of water

*kg/t clinker

cons14..          mass_H2O =e=

*Water from fossil fuels k

sum (k, (18/2)*fraction_h_k(k)*mass_foss(k)) +

*Water from non fossil fuels l

sum (l, (18/2)*fraction_h_l(l)*mass_nonfoss(l))

;

*Oxygen material balance

*kg/t clinker

cons15..         mass_O2 =e=

*Input air [23.2% O2; 76.8% N2]

0.232*m_air -

*Oxygen required for complete combustion of corresponding fossil fuels k

(sum (k, mass_foss(k)*St_O2_k(k))) -

*Oxygen required for complete combustion of corresponding non fossil fuels l

(sum (l, mass_nonfoss(l)*St_O2_l(l))) -

*Eliminating possibility of having N2 in input air

(sum (c, 0.232*n_oxy(c)*linearize_air(c))) +

*Pure O2 air feed

(sum (c, n_oxy(c)*linearize_oxygen(c)))

;

*O2 in flue gas is often controlled at a level of 10%

cons16..            mass_O2 =e= V_flue*(3.2/22.414)

;

*Nitrogen material balance

*kg/t clinker

cons17..         mass_N2 =e=

*Input air [23.2% O2; 76.8% N2]

0.768*m_air -

*Eliminating possibility of having N2 in input air (Pure O2 air feed)

(sum (c, 0.768*n_oxy(c)*linearize_air(c)))

;

*========================*

*HEAT CONSUMPTION IN KILN*

*========================*

*Heat consumed in kiln equals to heat contributed by fuels

*Heat needed by kiln equals to initial energy demand plus energy added or reduced by newly installed kiln r if chosen

*kJ/t clinker

cons18..          TED_Base*(1 - sum (r, XR(r)*effect_r(r))) =e=

*Heat contributed by fossil fuels k

sum (k, linearize_k(k)*NCV_k(k)) +

*Heat contributed by non fossil fuels l

sum (l, linearize_l(l)*NCV_l(l))

;

*==================*

*GENERAL TOTAL MASS*

*==================*

*kg/t clinker

cons19..            mass_fuels_used =e=

sum (k, mass_foss(k)) + sum (l, mass_nonfoss(l))

;

*kg/t clinker

cons20..            mass_raws_used =e=

sum (j, mass_raw(j))

;

*----------------------------------------------------------------------------------------------------------------------------------------------------------------------

* INEQUALITY CONSTRAINT * INEQUALITY CONSTRAINT * INEQUALITY CONSTRAINT * INEQUALITY CONSTRAINT * INEQUALITY CONSTRAINT * INEQUALITY CONSTRAINT * INEQUALITY CONSTRAINT

*----------------------------------------------------------------------------------------------------------------------------------------------------------------------

*=====================*

*CLINKER PHASE BALANCE*

*=====================*

*kg/t clinker

cons21..         Basis*LMC3S =l=

*From raw materials j

*From SiO2 in raw materials j

sum (j, (-7.6*SiO2_j(j)*mass_raw(j))

*From Al2O3 in raw materials j

- (6.72*Al2O3_j(j)*mass_raw(j))

*From Fe2O3 in raw materials j

- (1.43*Fe2O3_j(j)*mass_raw(j))

*From CaO in raw materials j

+ (4.07*CaO_j(j)*mass_raw(j))) +

*From fossil fuels k

*From SiO2 in ash from fossil fuels k

sum (k, (-7.6*SiO2_k(k)*ash_k(k)*mass_foss(k))

*From Al2O3 in ash from fossil fuels k

- (6.72*Al2O3_k(k)*ash_k(k)*mass_foss(k))

*From Fe2O3 in ash from fossil fuels k

- (1.43*Fe2O3_k(k)*ash_k(k)*mass_foss(k))

*From CaO in ash from fossil fuels k

+ (4.07*CaO_k(k)*ash_k(k)*mass_foss(k))) +

*From non fossil fuels l

*From SiO2 in ash from non fossil fuels l

sum (l, (-7.6*SiO2_l(l)*ash_l(l)*mass_nonfoss(l))

*From Al2O3 in ash from non fossil fuels l

- (6.72*Al2O3_l(l)*ash_l(l)*mass_nonfoss(l))

*From Fe2O3 in ash from non fossil fuels l

- (1.43*Fe2O3_l(l)*ash_l(l)*mass_nonfoss(l))

*From CaO in ash from non fossil fuels l

+ (4.07*CaO_l(l)*ash_l(l)*mass_nonfoss(l)))

;

*kg/t clinker

cons22..         Basis*UMC3S =g=

*From raw materials j

*From SiO2 in raw materials j

sum (j, (-7.6*SiO2_j(j)*mass_raw(j))

*From Al2O3 in raw materials j

- (6.72*Al2O3_j(j)*mass_raw(j))

*From Fe2O3 in raw materials j

- (1.43*Fe2O3_j(j)*mass_raw(j))

*From CaO in raw materials j

+ (4.07*CaO_j(j)*mass_raw(j))) +

*From fossil fuels k

*From SiO2 in ash from fossil fuels k

sum (k, (-7.6*SiO2_k(k)*ash_k(k)*mass_foss(k))

*From Al2O3 in ash from fossil fuels k

- (6.72*Al2O3_k(k)*ash_k(k)*mass_foss(k))

*From Fe2O3 in ash from fossil fuels k

- (1.43*Fe2O3_k(k)*ash_k(k)*mass_foss(k))

*From CaO in ash from fossil fuels k

+ (4.07*CaO_k(k)*ash_k(k)*mass_foss(k))) +

*From non fossil fuels l

*From SiO2 in ash from non fossil fuels l

sum (l, (-7.6*SiO2_l(l)*ash_l(l)*mass_nonfoss(l))

*From Al2O3 in ash from non fossil fuels l

- (6.72*Al2O3_l(l)*ash_l(l)*mass_nonfoss(l))

*From Fe2O3 in ash from non fossil fuels l

- (1.43*Fe2O3_l(l)*ash_l(l)*mass_nonfoss(l))

*From CaO in ash from non fossil fuels l

+ (4.07*CaO_l(l)*ash_l(l)*mass_nonfoss(l)))

;

*kg/t clinker

cons23..         Basis*LMC2S =l=

*From raw materials j

*From SiO2 in raw materials j

sum (j, (8.6*SiO2_j(j)*mass_raw(j))

*From Al2O3 in raw materials j

+ (5.07*Al2O3_j(j)*mass_raw(j))

*From Fe2O3 in raw materials j

+ (1.08*Fe2O3_j(j)*mass_raw(j))

*From CaO in raw materials j

- (3.07*CaO_j(j)*mass_raw(j))) +

*From fossil fuels k

*From SiO2 in ash from fossil fuels k

sum (k, (8.6*SiO2_k(k)*ash_k(k)*mass_foss(k))

*From Al2O3 in ash from fossil fuels k

+ (5.07*Al2O3_k(k)*ash_k(k)*mass_foss(k))

*From Fe2O3 in ash from fossil fuels k

+ (1.08*Fe2O3_k(k)*ash_k(k)*mass_foss(k))

*From CaO in ash from fossil fuels k

- (3.07*CaO_k(k)*ash_k(k)*mass_foss(k))) +

*From non fossil fuels l

*From SiO2 in ash from non fossil fuels l

sum (l, (8.6*SiO2_l(l)*ash_l(l)*mass_nonfoss(l))

*From Al2O3 in ash from non fossil fuels l

+ (5.07*Al2O3_l(l)*ash_l(l)*mass_nonfoss(l))

*From Fe2O3 in ash from non fossil fuels l

+ (1.08*Fe2O3_l(l)*ash_l(l)*mass_nonfoss(l))

*From CaO in ash from non fossil fuels l

- (3.07*CaO_l(l)*ash_l(l)*mass_nonfoss(l)))

;

*kg/t clinker

cons24..         Basis*UMC2S =g=

*From raw materials j

*From SiO2 in raw materials j

sum (j, (8.6*SiO2_j(j)*mass_raw(j))

*From Al2O3 in raw materials j

+ (5.07*Al2O3_j(j)*mass_raw(j))

*From Fe2O3 in raw materials j

+ (1.08*Fe2O3_j(j)*mass_raw(j))

*From CaO in raw materials j

- (3.07*CaO_j(j)*mass_raw(j))) +

*From fossil fuels k

*From SiO2 in ash from fossil fuels k

sum (k, (8.6*SiO2_k(k)*ash_k(k)*mass_foss(k))

*From Al2O3 in ash from fossil fuels k

+ (5.07*Al2O3_k(k)*ash_k(k)*mass_foss(k))

*From Fe2O3 in ash from fossil fuels k

+ (1.08*Fe2O3_k(k)*ash_k(k)*mass_foss(k))

*From CaO in ash from fossil fuels k

- (3.07*CaO_k(k)*ash_k(k)*mass_foss(k))) +

*From non fossil fuels l

*From SiO2 in ash from non fossil fuels l

sum (l, (8.6*SiO2_l(l)*ash_l(l)*mass_nonfoss(l))

*From Al2O3 in ash from non fossil fuels l

+ (5.07*Al2O3_l(l)*ash_l(l)*mass_nonfoss(l))

*From Fe2O3 in ash from non fossil fuels l

+ (1.08*Fe2O3_l(l)*ash_l(l)*mass_nonfoss(l))

*From CaO in ash from non fossil fuels l

- (3.07*CaO_l(l)*ash_l(l)*mass_nonfoss(l)))

;

*kg/t clinker

cons25..         Basis*LMC3A =l=

*From raw materials j

*From Al2O3 in raw materials j

sum (j, (2.65*Al2O3_j(j)*mass_raw(j))

*From Fe2O3 in raw materials j

- (1.69*Fe2O3_j(j)*mass_raw(j))) +

*From fossil fuels k

*From Al2O3 in ash from fossil fuels k

sum (k, (2.65*Al2O3_k(k)*ash_k(k)*mass_foss(k))

*From Fe2O3 in ash from fossil fuels k

- (1.69*Fe2O3_k(k)*ash_k(k)*mass_foss(k)))  +

*From non fossil fuels l

*From Al2O3 in ash from non fossil fuels l

sum (l, (2.65*Al2O3_l(l)*ash_l(l)*mass_nonfoss(l))

*From Fe2O3 in ash from non fossil fuels l

- (1.69*Fe2O3_l(l)*ash_l(l)*mass_nonfoss(l)))

;

*kg/t clinker

cons26..         Basis*UMC3A =g=

*From raw materials j

*From Al2O3 in raw materials j

sum (j, (2.65*Al2O3_j(j)*mass_raw(j))

*From Fe2O3 in raw materials j

- (1.69*Fe2O3_j(j)*mass_raw(j))) +

*From fossil fuels k

*From Al2O3 in ash from fossil fuels k

sum (k, (2.65*Al2O3_k(k)*ash_k(k)*mass_foss(k))

*From Fe2O3 in ash from fossil fuels k

- (1.69*Fe2O3_k(k)*ash_k(k)*mass_foss(k))) +

*From non fossil fuels l

*From Al2O3 in ash from non fossil fuels l

sum (l, (2.65*Al2O3_l(l)*ash_l(l)*mass_nonfoss(l))

*From Fe2O3 in ash from non fossil fuels l

- (1.69*Fe2O3_l(l)*ash_l(l)*mass_nonfoss(l)))

;

*kg/t clinker

cons27..         Basis*LMC4AF =l=

*From raw materials j

*From Fe2O3 in raw materials j

sum (j, (3.043*Fe2O3_j(j)*mass_raw(j))) +

*From fossil fuels k

*From Fe2O3 in ash from fossil fuels k

sum (k, (3.043*Fe2O3_k(k)*ash_k(k)*mass_foss(k))) +

*From non fossil fuels l

*From Fe2O3 in ash from non fossil fuels l

sum (l, (3.043*Fe2O3_l(l)*ash_l(l)*mass_nonfoss(l)))

;

*kg/t clinker

cons28..         Basis*UMC4AF =g=

*From raw materials j

*From Fe2O3 in raw materials j

sum (j, (3.043*Fe2O3_j(j)*mass_raw(j))) +

*From fossil fuels k

*From Fe2O3 in ash from fossil fuels k

sum (k, (3.043*Fe2O3_k(k)*ash_k(k)*mass_foss(k))) +

*From non fossil fuels l

*From Fe2O3 in ash from non fossil fuels l

sum (l, (3.043*Fe2O3_l(l)*ash_l(l)*mass_nonfoss(l)))

;

*=========================*

*THERMAL SUBSTITUTION RATE*

*=========================*

*Heat contributed by alternative fuels must not be more than the specific upper limit of total energy limit (TSR)

*TSR value used is 30%

*kJ/t clinker

cons29..         TSR*TED_Base*(1 - sum (r, XR(r)*effect_r(r))) =g=

sum (l, linearize_l(l)*NCV_l(l))

;

*=======================================*

********CO2 REDUCTION CONSTRAINT*********

*=======================================*

*Only CO2 produce from non biogenic fuels and raw materials are considered in reduction target

*CO2 reduction target used is 10% from total of carbon dioxide produce <-------- Can be used for sensitivity analysis

*kg/t clinker

cons30..         CCO2*(1 - CO2_Target) =g=

*Mass of CO2 emitted from clinkerization, and burning of fuels k and l

CO2_released

;

*==================*

*FUELS AVAILABILITY*

*==================*

*Availability constraints on primary fuels

cons31(k)..         mass_foss(k) =l= 5000000*XK(k)

;

*Availability constraints on alternative fuels

cons32(l)..         mass_nonfoss(l) =l= 5000000*XL(l)

;

*===================*

*EXACT LINEARIZATION*

*===================*

*Where linearize_l(l) = XL(l)*mass_nonfoss(l)

cons33(l)..         linearize_l(l) =l= mass_nonfoss(l)

;

cons34(l)..         linearize_l(l) =g= mass_nonfoss(l) - (60000)*(1 - XL(l))

;

cons35(l)..         linearize_l(l) =l= 60000*XL(l)

;

cons36(l)..         linearize_l(l) =g= 0

;

*Where linearize_k(k) = XK(k)*mass_foss(k)

cons37(k)..         linearize_k(k) =l= mass_foss(k)

;

cons38(k)..         linearize_k(k) =g= mass_foss(k) - (60000)*(1 - XK(k))

;

cons39(k)..         linearize_k(k) =l= 60000*XK(k)

;

cons40(k)..         linearize_k(k) =g= 0

;

*Where linearize_c(c) = XC(c)*nonbio_CO2

cons41(c)..         linearize_c(c) =l= nonbio_CO2

;

cons42(c)..         linearize_c(c) =g= nonbio_CO2 - (2000)*(1 - XC(c))

;

cons43(c)..         linearize_c(c) =l= 2000*XC(c)

;

cons44(c)..         linearize_c(c) =g= 0

;

*Where linearize_air(c) = XC(c)*m_air

cons45(c)..         linearize_air(c) =l= m_air

;

cons46(c)..         linearize_air(c) =g= m_air - (4000)*(1 - XC(c))

;

cons47(c)..         linearize_air(c) =l= 4000*XC(c)

;

cons48(c)..         linearize_air(c) =g= 0

;

*Where linearize_oxygen(c) = XC(c)*m_oxygen

cons49(c)..         linearize_oxygen(c) =l= m_oxygen

;

cons50(c)..         linearize_oxygen(c) =g= m_oxygen - (1)*(4000 - XC(c))

;

cons51(c)..         linearize_oxygen(c) =l= 4000*XC(c)

;

cons52(c)..         linearize_oxygen(c) =g= 0

;

cons53..             CO2_nonbio_altfuel =e=

*Mass of CO2 produced by the burning of non fossil fuels l

sum (l, (1 - anthro_l(l))*CEF_l(l)*linearize_l(l))

;

cons54..              CO2_nonbio_fossfuel =e= sum (k, (1 - anthro_k(k))*CEF_k(k)*linearize_k(k));

cons55..              oxygen_used =e= (sum (k, mass_foss(k)*St_O2_k(k))) + (sum (l, mass_nonfoss(l)*St_O2_l(l)))           ;

cons56..              oxygen_feed =e= 0.232*m_air;

cons57..              CO2_captured =e= nonbio_CO2 - CO2_released;

cons58(j)..           cost_raws(j) =e=  Cost_Raw(j)*mass_raw(j);

cons59..              total_raws =e= sum (j, cost_raws(j));

cons60(k)..           cost_fossil(k) =e=  Cost_Foss(k)*mass_foss(k);

cons61..              total_fossil =e= sum (k, cost_fossil(k));

cons62(l)..           cost_nonfossil(l) =e= Cost_NonFoss(l)*mass_nonfoss(l);

cons63..              total_nonfossil =e= sum (l, cost_nonfossil(l));

cons64..              cost_coprocess =e= sum (l, ((correlate*XL(l)*Cost_fuel_FCI(l)/AC) + (Cost_fuel_VC(l)*mass_nonfoss(l))));

cons65..              cost_kiln =e= sum (r, (correlate*XR(r)*Cost_kiln_FCI(r)));

cons66..              cost_ccs =e= sum (c, ((correlate*Amor*Cost_ccs_FCI(c)*XC(c)/AC) + (correlate*Cost_ccs_VC(c)*XC(c)/AC))) ;

cons67..              plant_cost =e= correlate*Amor*FCI/AC + correlate*OC/AC ;

cons68..              total_fuel =e= total_fossil + total_nonfossil + cost_coprocess;

cons69..              nonfossil_overall =e= total_nonfossil + cost_coprocess;

cons70..              thermal_1 =e=

sum (k, linearize_k(k)*NCV_k(k)) +

*Heat contributed by non fossil fuels l

sum (l, linearize_l(l)*NCV_l(l))   ;

cons71..              thermal_2 =e=

1000000*(sum (k, linearize_k(k)*NCV_k(k)) +

*Heat contributed by non fossil fuels l

sum (l, linearize_l(l)*NCV_l(l)))   ;

cons72..               C3S =e=

*From raw materials j

*From SiO2 in raw materials j

sum (j, (-7.6*SiO2_j(j)*mass_raw(j))

*From Al2O3 in raw materials j

- (6.72*Al2O3_j(j)*mass_raw(j))

*From Fe2O3 in raw materials j

- (1.43*Fe2O3_j(j)*mass_raw(j))

*From CaO in raw materials j

+ (4.07*CaO_j(j)*mass_raw(j))) +

*From fossil fuels k

*From SiO2 in ash from fossil fuels k

sum (k, (-7.6*SiO2_k(k)*ash_k(k)*mass_foss(k))

*From Al2O3 in ash from fossil fuels k

- (6.72*Al2O3_k(k)*ash_k(k)*mass_foss(k))

*From Fe2O3 in ash from fossil fuels k

- (1.43*Fe2O3_k(k)*ash_k(k)*mass_foss(k))

*From CaO in ash from fossil fuels k

+ (4.07*CaO_k(k)*ash_k(k)*mass_foss(k))) +

*From non fossil fuels l

*From SiO2 in ash from non fossil fuels l

sum (l, (-7.6*SiO2_l(l)*ash_l(l)*mass_nonfoss(l))

*From Al2O3 in ash from non fossil fuels l

- (6.72*Al2O3_l(l)*ash_l(l)*mass_nonfoss(l))

*From Fe2O3 in ash from non fossil fuels l

- (1.43*Fe2O3_l(l)*ash_l(l)*mass_nonfoss(l))

*From CaO in ash from non fossil fuels l

+ (4.07*CaO_l(l)*ash_l(l)*mass_nonfoss(l)))

;

cons73..         C2S =e=

*From raw materials j

*From SiO2 in raw materials j

sum (j, (8.6*SiO2_j(j)*mass_raw(j))

*From Al2O3 in raw materials j

+ (5.07*Al2O3_j(j)*mass_raw(j))

*From Fe2O3 in raw materials j

+ (1.08*Fe2O3_j(j)*mass_raw(j))

*From CaO in raw materials j

- (3.07*CaO_j(j)*mass_raw(j))) +

*From fossil fuels k

*From SiO2 in ash from fossil fuels k

sum (k, (8.6*SiO2_k(k)*ash_k(k)*mass_foss(k))

*From Al2O3 in ash from fossil fuels k

+ (5.07*Al2O3_k(k)*ash_k(k)*mass_foss(k))

*From Fe2O3 in ash from fossil fuels k

+ (1.08*Fe2O3_k(k)*ash_k(k)*mass_foss(k))

*From CaO in ash from fossil fuels k

- (3.07*CaO_k(k)*ash_k(k)*mass_foss(k))) +

*From non fossil fuels l

*From SiO2 in ash from non fossil fuels l

sum (l, (8.6*SiO2_l(l)*ash_l(l)*mass_nonfoss(l))

*From Al2O3 in ash from non fossil fuels l

+ (5.07*Al2O3_l(l)*ash_l(l)*mass_nonfoss(l))

*From Fe2O3 in ash from non fossil fuels l

+ (1.08*Fe2O3_l(l)*ash_l(l)*mass_nonfoss(l))

*From CaO in ash from non fossil fuels l

- (3.07*CaO_l(l)*ash_l(l)*mass_nonfoss(l)))

;

cons74..         C3A =e=

*From raw materials j

*From Al2O3 in raw materials j

sum (j, (2.65*Al2O3_j(j)*mass_raw(j))

*From Fe2O3 in raw materials j

- (1.69*Fe2O3_j(j)*mass_raw(j))) +

*From fossil fuels k

*From Al2O3 in ash from fossil fuels k

sum (k, (2.65*Al2O3_k(k)*ash_k(k)*mass_foss(k))

*From Fe2O3 in ash from fossil fuels k

- (1.69*Fe2O3_k(k)*ash_k(k)*mass_foss(k)))  +

*From non fossil fuels l

*From Al2O3 in ash from non fossil fuels l

sum (l, (2.65*Al2O3_l(l)*ash_l(l)*mass_nonfoss(l))

*From Fe2O3 in ash from non fossil fuels l

- (1.69*Fe2O3_l(l)*ash_l(l)*mass_nonfoss(l)))

;

cons75..         C4AF =e=

*From raw materials j

*From Fe2O3 in raw materials j

sum (j, (3.043*Fe2O3_j(j)*mass_raw(j))) +

*From fossil fuels k

*From Fe2O3 in ash from fossil fuels k

sum (k, (3.043*Fe2O3_k(k)*ash_k(k)*mass_foss(k))) +

*From non fossil fuels l

*From Fe2O3 in ash from non fossil fuels l

sum (l, (3.043*Fe2O3_l(l)*ash_l(l)*mass_nonfoss(l)))

;

*Fixed capital cost

cons76..       capital =e=

*Capital cost

(correlate*Amor*FCI/AC +

*Retrofitting cost (fuel switching + kiln + CCS retrofitting)

*Kiln

sum (r, (correlate*XR(r)*Cost_kiln_FCI(r))) +

*Fuel switching cost

sum (l, (correlate*XL(l)*Cost_fuel_FCI(l)/AC)) +

*CCS installation

sum (c, (correlate*Amor*Cost_ccs_FCI(c)*XC(c)/AC)))

;

*Annual cost (€/yr)

cons77..       annual =e=

*Operating cost

(correlate*OC/AC +

*Raw materials j cost

sum (j, Cost_Raw(j)*mass_raw(j)) +

*Fossil fuels k cost

sum (k, Cost_Foss(k)*mass_foss(k)) +

*Non fossil fuels l cost

sum (l, Cost_NonFoss(l)*mass_nonfoss(l)) +

*Retrofitting cost (fuel switching + kiln + CCS retrofitting)

*Fuel switching cost

sum (l, (Cost_fuel_VC(l)*mass_nonfoss(l)) +

*CCS installation

sum (c, (correlate*Cost_ccs_VC(c)*XC(c)/AC))))

;

MODEL            Project /all/;

Option optca=0;

Option optcr=0;

SOLVE            Project using MINLP minimizing min_cost;

DISPLAY

*CCO2.l,

min_cost.l, annual.l, capital.l, cost_raws.l, total_raws.l, cost_fossil.l, total_fossil.l, cost_nonfossil.l, total_nonfossil.l, total_fuel.l, nonfossil_overall.l, cost_coprocess.l, cost_kiln.l, cost_ccs.l, plant_cost.l,

m_oxides.l, m_alkalis.l, m_sulfurs.l, m_metals.l, mass_clinker_produced.l,

C3S.l, C2S.l, C3A.l, C4AF.l,

mass_raws_used.l, mass_raw.l, mass_fuels_used.l, mass_foss.l, mass_nonfoss.l,

thermal_1.l, thermal_2.l, produced_CO2.l, bio_CO2.l, nonbio_CO2.l, CO2_nonbio_altfuel.l, CO2_nonbio_fossfuel.l, m_clink.l, CO2_captured.l, CO2_released.l,

V_flue.l, m_flue_g.l, m_air.l, mass_N2.l, oxygen_feed.l, mass_H2O.l, mass_O2.l, m_oxygen.l, oxygen_used.l,

XK.l, XL.l, XR.l, XC.l, linearize_k.l, linearize_l.l, linearize_c.l;

*cons30 - cons51 for basis 1000, 10 zeroes

*cons __ __ for increase rate, __ zeroes